## Slide 1
TRANSPORTATION
IMPROVEMENT
BOARD
OTTA SEAL
Using High Float Emulsions
(HF-150)

## Slide 2
What is Otta Seal?
Otta Seal is a surface treatment that uses a medium of rock that interlocks with each other like hotmix. It is made by placing the rock medium on top of a thick application of relatively soft, bituminous binding agent such as HF-1501. Otta Seal can look like gravel after immediate installation, but over time the black oils will work their way up creating the appearance of a normally paved surface.
Transportation Improvement Board | Otta Seal Overview
1Johnson, G., & Pantelis, J. 2003, 2008. Otta Seal Surfacing of Aggregate Roads. http://www.dot.state.mn.us/materials/bituminousdocs/Pavement%20Maintenance/OttaSeal_4-pagerMRR_2008.pdf

## Slide 3
Recap of Chip Seal
Chip Seal is one layer of clean rock that requires enough oil to secure it. It is one of the oldest and most common street-surfacing methods1.
Transportation Improvement Board | Chip Seal Overview
1Chip Seal Brochure. https://static.spokanecity.org/documents/projects/2021-residential-chip-seal/chip-seal-brochure.pdf

## Slide 4
Transportation Improvement Board | Otta Seal Advantages
Advantages of Otta Seal
Otta Seal
  Costs less than washed rock, saving money for agencies
  Less brittle at low temperatures, less prone to temperature related failure
  Does not bleed like base AC emulsions
  Holds rock medium better
  Fines in the rock can fill in cracks and voids
  Otta seal can last 8 to 15 years or more with proper maintenance
Chip Seal
  While effective, the medium is more expensive and less accessible to smaller agencies and communities
  More susceptible to weather and traffic damage
  Lasts about half the lifespan of Otta seal
Asphalt Surfacing. https://web.archive.org/web/20120426011304/http://www.cflhd.gov/programs/techDevelopment/pavement/context-roadway-
surfacing/documents/roadway-surfacing-photos/ch1-c-asphalt.pdf
Johnson, G., & Pantelis, J. 2003, 2008. Otta Seal Surfacing of Aggregate Roads. http://www.dot.state.mn.us/materials/bituminousdocs0
/Pavement%20Maintenance/OttaSeal_4-pagerMRR_2008.pdf

## Slide 5
Process for Single Shot Otta Seal on
Paved Surface
Step One
Lay down materials
  Apply oil
  Allow oil to penetrate
  Apply cover stone
Step Two
Roll with two rollers
  One roller should be a steal drum
  This seals the treatment
Step Three
Return after three weeks and sweep excess rock
Transportation Improvement Board | Single Shot on Paved Surface
Photos from Creston, WA Otta Seal Project!

## Slide 6
Step One
Lay down materials
  Apply oil
  Allow oil to penetrate
  Apply cover stone
Step Two
Roll with two rollers
  One roller should be a steal drum
  This seals the treatment
Step Three
After 7-10 days, apply second layer of materials
  Place with oil
  Apply cover stone
Step Four
Return after three weeks and sweep excess rock
Transportation Improvement Board | Double Shot on Gravel Surface
Process for Double Shot Otta Seal on
Gravel Surface

## Slide 7
Differences in Oils
Transportation Improvement Board | Differences in Oils
High Float Emulsion (HF-150)
  Easier to handle than cationic oils
  More forgiving emulsion
  Works well with crushed stone aggregate
  Saves money due to materials used
Conventional Emulsions
  Sets much more quickly
  Relies on kerosene evaporation
  Works with more expensive, washed aggregate

## Slide 8
Crushed Cover Stone
30 - 35
Undiluted Asphalt (gal/sy)
Aggregate Application
(lbs/sy)
Aggregate Size
0.45 - 0.50
Application Rate for Otta Seal on
Paved Surface
  Apply 0.45-0.50 gal/sy HF-150 to compacted gravel surface.
  Let it penetrate.
  Apply 30-35 lbs/sy cover stone.
  Due to low volume traffic, ensure extra rolling effort with two rollers (at least one shall be a steel drum) to seat the cover.
  Optional- After 3 weeks of placement, sweep excess rock.
Process for Otta Seal on a Paved Surface
Transportation Improvement Board | Otta Seal on a Paved Surface

## Slide 9
Crushed Cover Stone
30 - 35
Undiluted Asphalt (gal/sy)
Aggregate Application
(lbs/sy)
Aggregate Size
0.45 - 0.50
Application Rate for Otta Seal on
Gravel Surface
  Apply 0.45-0.50 gal/sy HF-150 to compacted gravel surface.
  Let it penetrate.
  Apply 30-35 lbs/sy cover stone.
  Due to low volume traffic, ensure extra rolling effort with two rollers (at least one shall be a steel drum) to seat the cover.
  The second application should be applied 7-10 days after the first application.
Process for Otta Seal on a Surface
Transportation Improvement Board | Otta Seal on a Gravel Surface
First Application
Second Application
Crushed Cover Stone
30 - 32
0.40 - 0.44
  Second application- Seal again with 0.40-0.44 gal/sy HF-150
  Apply 30-32 lbs/sy cover stone.
  Again, extra rolling effort which includes a steel drum roller.
  Optional- After 3 weeks of placement of second application, sweep excess rock.

## Slide 10
Additional Specifications
Crushed Cover Stone Specifications
3/4” Square Sieve
5/8” Square Sieve
No. 4
No. 200
% Fracture by weight, min.
Sand Equivalent
Static Stripping Test
100% passing
95-100% passing
20-45% passing
0-7.5% passing
75%
40 min
Pass
Test
Requirement
Oil Specifications for HFE-150
130
175
Min. F
Max. F